| TID | ATLAS STANDARD TID TEST REPORT revision 3 (12-Jun-01) | Page 1/5 Ref. DB: |
| --- | --- | --- |

# Please complete and submit this ATLAS Standard Form to ATLAS RHA Coordinator (ARC),

# at least 2 weeks after the date of the test.

1. General information:

| 1.1 | Date of the test: | 12/12/02 |
| --- | --- | --- |
| 1.2 | Pre-selection, or Qualification ? (specify) | Pre-selection |
| 1.3 | Name of the ATLAS (or other) System: | TGC |
| 1.4 | Name of the board in the System: | Star Switch Board |
| 1.5 | Person responsible for the test: | Osamu Sasaki |
| 1.6 | Institute: | KEK |
| 1.7 | Email: | osamu.sasaki@kek.jp |
| 1.8 | Person responsible for RHA of the Board: | Osamu Sasaki |
| 1.9 | Institute: | KEK |
| 1.10 | Email: | osamu.sasaki@kek.jp |

2. Component:

| 2.1 | Name: | Anti-Fuse FPGA |
| --- | --- | --- |
| 2.2 | Part Number: | AX250 |
| 2.3 | Type (see section 10.1): | Logic |
| 2.4 | Function (see section 10.1): | Anti-Fuse FPGA |
| 2.5 | Main specification of the component: Anti-Fuse FPGA, memory. |
| 2.6 | Design (specify: COTS/ASIC): | COTS |
| 2.7 | Design center (if known): |  |
| Manufacturer: |  |
| 2.8 | Name of the manufacturer: | Actel |
| 2.9 | Address of the manufacturer (if known): |  |
| 2.10 | Phone of the manufacturer (if known): |  |
| 2.11 | Email of the manufacturer (if known): |  |
| 2.12 | Web URL of the manufacturer (if known): | http://www.actel.com |
| Sampling: |  |
| 2.13 | Number of tested components (irradiated): | 4(gamma), 4(proton) |
| 2.14 | Number of reference components (un-irradiated): |  |
| Batch origin: |  |
| 2.15 | Batch origin (Homogeneous/Unknown): |  |
| 2.16 | Manufacturing date code (for homogeneous batch): |  |
| 2.17 | Manufacturing line code (for homogeneous batch): |  |
| Technology: |  |
| 2.18 | Name of the technology (if known): |  |
| 2.19 | Technology (CMOS/BiCMOS/Bipolar/AsGa/Other): | CMOS |
| 2.20 | Minimum geometry (m) : |  |
| Package: |  |
| 2.21 | Type: | QFP |
| 2.22 | Part number: |  |
| 2.23 | Number of pin: | 208 |
| 2.24 | Ceramic ? Plastic ? hybrid ? (specify) | Plastic |

| TID | ATLAS STANDARD TID TEST REPORT revision 3 (12-Jun-01) | Page 2/5 Ref. DB: |
| --- | --- | --- |

3. Radiation:

| 3.1 | Name of the radiation facility: | RCNST(gamma, Univ. of Tokyo), CYRIC(proton, Tohoku Univ.) |
| --- | --- | --- |
| 3.2 | Address of the radiation facility: | Hongo Tokyo, Sendai Miyagi Japan |
| 3.3 | Radiation source (see 12.2) : | Co-60, Cyclotron |
| 3.4 | Radiation type (see 12.2) : | Photon gamma, proton |
| 3.5 | Radiation energy: | 1.173, 1.332MeV gamma, 70 MeV proton |
| 3.6 | Dose rate (Gray/s) : | 0.19 Gray/s (gamma), <0.8 Gray/s (proton) |
| 3.7 | Total dose after last step (Gray) : | 1.8 kGray (gamma), 1.2 kGray (proton) |
| 3.8 | NIEL (if any) after last step (1 MeV eq. n/cm2) : |  |
| 3.9 | Dosimetry / Calibration method: |  |

4. Radiation test method (see 12.3):  (put an “X” to designate your answer. Specify in 4.10 if necessary)

| 4.1 | Extended TID test method for pre-selection of CMOS devices? |  |
| --- | --- | --- |
| 4.2 | Simplified TID test method for pre-selection of CMOS devices? | X () |
| 4.3 | Extended TID test method for pre-selection of bipolar devices? |  |
| 4.4 | Simplified TID test method for pre-selection of bipolar devices? |  |
| 4.5 | Extended TID test method for qualification of CMOS batches? |  |
| 4.6 | Simplified TID test method for qualification of CMOS batches? |  |
| 4.7 | Extended TID test method for qualification of bipolar or BiCMOS batches? |  |
| 4.8 | Simplified TID test method for qualification of bipolar or BiCMOS batches? |  |
| 4.9 | Other TID test method? | X(proton) |
| 4.10 | Which other TID test method (specify) ? Proton beam irradiation and online measurement, no annealing, no aging. |

5. Total dose: (if the irradiation is made in one single step, answer to question 5.1 and 5.2 only)

| 5.1 | Total number of irradiation steps: |  |
| --- | --- | --- |
| 5.2 | TID (Gray) after step 1: | 1.4 kGy (Gamma), 900 Gy (proton) |
| 5.3 | TID (Gray) after step 2 (if more than one step): |  |
| 5.4 | TID (Gray) after step 3 (if more than two steps): |  |
| 5.5 | TID (Gray) after step 4 (if more than three steps): |  |
| 5.6 | TID (Gray) after step 5 (if more than four steps): |  |
| 5.7 | TID (Gray) after step 6 (if more than five steps): |  |

6. Simulation of Low Dose Rate Effects (see 12.4):

| Bipolar devices only: |  |
| --- | --- |
| 6.1 | Did you perform irradiation at elevated temperature to simulate low dose rate effects (Y/N) ? |  |
| 6.2 | If “yes” to Q.6.1, how much irradiation pre-tests did you perform to determine the worst case temperature? |  |
| 6.3 | If “yes” to Q.6.1, what is the worst temperature determined from pre-tests (oC)? |  |
| 6.4 | If “no” to Q.6.1, which safety factor do you use to represent low dose rate effects? |  |
| CMOS and BiCMOS only: |  |
| 6.5 | Did you perform post-irradiation aging to simulate low dose rate effects (Y/N) ? | N |
| 6.6 | If “no” to Q.6.5, which safety factor do you use to represent low dose rate effects? |  |

| TID | ATLAS STANDARD TID TEST REPORT revision 3 (12-Jun-01) | Page 3/5 Ref. DB: |
| --- | --- | --- |

7. Thermal and voltage stresses:

| During irradiation: |  |
| --- | --- |
| 7.1 | Temperature (oC) ? | 25oC |
| 7.2 | Supply voltage (Y/N) ? | Y |
| 7.3 | If “yes” to 7.2, value of supply voltage: | 3.3 V, 1.5V |
| 7.4 | AC operation (Y/N) ? | Y |
| 7.5 | If “yes” to 7.4, which AC operation? Ring oscillator and shift registers running, read memories and shift registers. |
| 7.6 | If “yes” to 7.4, which frequency? | 10MHz |
| During post irradiation annealing: |  |
| 7.7 | Did you perform post-irradiation annealing (Y/N) ? | Y(gamma only) |
| 7.8 | If “yes” to 7.7, annealing temperature (oC) ? | oC |
| 7.9 | If “yes” to 7.7, duration? | 3 minites per each chip |
| 7.10 | If “yes” to 7.7, supply voltage (Y/N) ? | Y |
| 7.11 | If “yes” to 7.7 and 7.10, which supply voltage? |  |
| 7.12 | If “yes” to 7.7, AC operation (Y/N) ? |  |
| 7.13 | If “yes” to 7.7 and 7.12, which AC operation? |  |
| 7.14 | If “yes” to 7.7 and 7.12, which AC frequency? |  |
| During post irradiation accelerated aging: |  |
| 7.15 | Did you perform post-irradiation ageing (Y/N) ? | N |
| 7.16 | If “yes” to 7.15, aging temperature (oC) ? |  |
| 7.17 | If “yes” to 7.15, duration? |  |
| 7.18 | If “yes” to 7.15, supply voltage (Y/N) ? |  |
| 7.19 | If “yes” to 7.15 and 7.18, which supply voltage? |  |
| 7.20 | If “yes” to 7.15, AC operation (Y/N) ? |  |
| 7.21 | If “yes” to 7.15 and 7.20, which AC operation? |  |
| 7.22 | If “yes” to 7.15 and 7.20, which AC frequency? |  |

8. Electrical measurement:

| During irradiation: |  |
| --- | --- |
| 8.1 | Did you perform on-line measurement (Y/N) ? | Y |
| 8.2 | If “yes” to 8.1, at which temperature (oC) ? | 25oC |
| 8.3 If “yes” to 8.1, describe on-beam operation and measurements: Ring Oscillator and read out 4-bit x 345 shift registers and 12 memories (12 x 9-bit x 512). |
| After irradiation: |  |
| 8.4 | Did you perform electrical measurements just after irradiation (Y/N) ? |  |
| 8.5 | Duration between irradiation and electrical measurement? |  |
| 8.6 | Temperature during electrical measurement (oC) ? | oC |
| After annealing: |  |
| 8.7 | Did you perform electrical measurements after annealing (Y/N) ? |  |
| 8.8 | Duration between annealing and electrical measurement? |  |
| 8.9 | Temperature during electrical measurements? | oC |

| TID | ATLAS STANDARD TID TEST REPORT revision 3 (12-Jun-01) | Page 4/5 Ref. DB: |
| --- | --- | --- |

8. Electrical measurement (cont.):

| After accelerated aging: |  |
| --- | --- |
| 8.10 | Did you perform electrical measurements after aging (Y/N) ? |  |
| 8.11 | Duration between aging and electrical measurement? |  |
| 8.12 | Temperature during electrical measurement (oC) ? |  |
| Description of off-line measurements (after irradiation; after annealing or after aging): |

9. Rejection criteria:

|  | Measured parameter | Rejection Criteria |
| --- | --- | --- |
| 9.1 |  |  |
| 9.2 |  |  |
| 9.3 |  |  |
| 9.4 |  |  |
| 9.5 |  |  |

10. Results:

|  | 10.1 | 10.2 | 10.3 | 10.4 | 10.5 | 10.6 |
| --- | --- | --- | --- | --- | --- | --- |
|  | Serial number of the device under test | Max. applied total dose (Gy) | Failure dose (Gy) if any failure during irradiation | Failure during annealing (Y/N)? | Failure during ageing (Y/N)? | Failure mechanism (if any): for component “dead” or out of specification, give explanations and numbers |
| 1 | Boad0 chip0() | 330 | N | N |  |  |
| 2 | Board0 chip1() | 330 | N | N |  |  |
| 3 | Board 1 chip0() | 1360 | N | N |  |  |
| 4 | Boad1 chip1() | 1360 | N | N |  |  |
| 5 | Board0 chip0(p) | 600 | N |  |  |  |
| 6 | Board0 chip1(p) | 590 | N |  |  |  |
| 7 | Board1 chip0(p) | 930 | N |  |  |  |
| 8 | Board1 chip1(p) | 920 | N |  |  |  |
| 9 |  |  |  |  |  |  |
| 10 |  |  |  |  |  |  |
| 11 |  |  |  |  |  |  |
| 12 |  |  |  |  |  |  |
| 13 |  |  |  |  |  |  |
| 14 |  |  |  |  |  |  |
| 15 |  |  |  |  |  |  |
| 16 |  |  |  |  |  |  |
| 17 |  |  |  |  |  |  |
| 18 |  |  |  |  |  |  |
| 19 |  |  |  |  |  |  |
| 20 |  |  |  |  |  |  |

| TID | ATLAS STANDARD TEST REPORT revision 3 (12-Jun-01) | Page 5/5 Ref. DB: |
| --- | --- | --- |

11. Comments

Use the space below to comment test results, or to report them if the above-dedicated space is inappropriate for you.

12. Guidelines

12.1 Type and Function

| Type | Function |
| --- | --- |
| Analogue device | ADC; Analogue memory; Analogue multiplexor; DAC; LVDS driver; LVDS receiver; Modulator/Demodulator; Voltage/Frequency converter |
| Data transmission Component | Receiver; Transceiver; Transmitter |
| Front-end electronic device | Drift Time Measurement; Multiple functions; Readout memory |
| Linear device | Amplifier; Comparator; Operational amplifier; Voltage reference; |
| Memory | SRAM |
| Microprocessor or peripheral | Microcontroller; Microprocessor |
| Optoelectronic component | Laser; Light emitting diode – LED; PIN diode; VCSEL |
| Power device | DC-DC converter; Power transistor; Voltage regulator |
| Programmable device | EEPROM; FPGA; Lookup table; Programmable delay |
| Passive component | Capacitor |
| Interfaces/Communication | LVDS; Switch |
| Mixed A/D device | Multiple functions |
| Logic gates | NOR, NAND, etc. |

12.2 Radiation source and type

| Source of radiation | Type of radiation |
| --- | --- |
| Accelerator | Electron, proton, spallation neutron |
| Am-241 | Ions (fission products) |
| Cf-252 | Ions (fission products) |
| Co-60 | Photon gamma 1.173 MeV and 1.332 MeV |
| Cs-137 | Photon gamma 0.662 MeV |
| Cyclotron | Proton, ion (specify), spallation neutron |
| Reactor | Neutron |
| Tandem accelerator | Protons, ions |
| Van-de-Graaf | Electron |
| X-Ray generator | Photon X |

12.3	Radiation test methods:

see ATLAS Policy on Radiation Tolerant Electronics rev. 2, pp. 20-26 http://atlas.web.cern.ch/Atlas/GROUPS/FRONTEND/WWW/RAD/RadWebPage/ATLASPolicy/APRTE_rev2_250800.pdf

12.4	Low dose rate effects:

see ATLAS Policy on Radiation Tolerant Electronics rev. 2, pp. 11 http://atlas.web.cern.ch/Atlas/GROUPS/FRONTEND/WWW/RAD/RadWebPage/ATLASPolicy/APRTE_rev2_250800.pdf